FIRE PROTECTION OF DOORS – general guidelines

Important - Please refer this explanation, as part of your Specification for the door upgrade, to the Authority that is asking for Fire Protection. This will help them to decide if they will allow you to upgrade the type of door that is installed.

Background

Due to the hugely varying nature of doors and their construction, it is impractical and misleading to carry out NAMAS/UKAS Laboratory fire door testing, because each individual door would have to be assessed on its own merits. The cost of such testing is uneconomic, because of the vast number of door variables.

The great majority of doors, including ALL hollow doors, are unsuitable for upgrading to 30, or even 20 mins Fire Resistance. There are however, certain well constructed, solid and substantial doors capable of being upgraded with our Intumescent Fire Varnish, as this is by far the most effective clear Fire treatment or coating available today.

Generally, suitable doors will be hardwood, or solid softwood with hardwood veneer. Intumescent paint (white or coloured) is capable of significantly greater Fire Resistance than Varnish, per coat. If you have softwood doors, we suggest you refer to our "Fire Door Paint" information sheet.

Our Fire Varnish Class ‘O’ Part 6 Fire Propagation Test showed that protected softwood did not burn within the 10 minutes test duration.

Further in-house testing indicated that when applied at twice the Class ‘O’ specified coating thickness, our Intumescent Fire Varnish added a further 15 mins Fire Resistance.

We assess door upgrade jobs requiring 30 minutes of Fire Resistance on an individual basis, referring to the above, TRADA Char Rate Tables and calculated residual timber to ascertain whether we could issue a Fire Certificate for the project.

SOFTWOOD DOORS

In order to issue a 30 mins Fire Certificate, in the case of softwood, the surface must be able to afford the loss of 10 mm depth from all surfaces exposed to a fire.

In other words, the residual timber should be adequate after such loss to avoid premature collapse, splitting or cracking, ensuring that neither flames nor the substantial heat required to promote combustion can pass through the door.

In general terms, few modern softwood doors can be protected with confidence. Old Pitch Pine & other very well seasoned softwood doors can be protected, but only if the frame can withstand a 10mm loss. In these cases panels less than 10mm thick should be supplemented by inserting an additional panel to take the total panel thickness to 10mm, trapping the additional panel behind the door's beading.

Substantial, solid doors unable to afford the loss of 10mm to the frame can achieve 20 minutes with the 30 minute specification as below.

OAK & OTHER RESISTANT HARDWOOD DOORS

In the case of oak or similar timbers, the required loss from charring to take into account is 6 mm.

These types, including modern oak-faced doors with solid compressed core, with frames 35mm+ thick, can be upgraded to 30 minutes. Any inset panel less than 10mm thick should be supplemented by an additional panel, trapped by the door's beading, to take overall panel thickness to 10mm+.

WHICH SIDE TO PROTECT?

Generally, the room side of doors should be coated, to protect the corridor and stairwell coming from potential fire in a room. Where it is felt the doors should have some protection on the corridor side, in order to avoid the doors themselves creating a fire hazard, a sensible approach, adopted by some Authorities, is to have the doors treated to

Class ‘O’ Standard, thus complying with flame spread and fire propagation Standards for general surfaces within corridors, stairways and other "means of escape". If a door divides a corridor, or divides a corridor from a stairwell, it should be treated to the full 30 Minutes specification on both sides.

30 Mins Fire Resistance Specification (20 mins in case of some softwood doors, as referred to above)

2 coats of Intumescent Fire Varnish at 6.5 sq.m/litre, per coat

1 coat Fire Varnish Overcoat at 10-12 sq.m/litre, per coat (2 coats on areas of high wear, or requiring frequent cleaning)

EXAMPLE OF APPROXIMATE COVERAGES - 30/20 mins (as above) - allows for number of coats necessary.

A 20sq.m pack of Intumescent Fire Varnish will cover 3 door sides, plus frame (at Class ‘O’ will cover 8 door sides and frames)

A 2.5 litres of Fire Varnish Overcoat will cover 8 door sides, plus frame

For prices, Next Working Day Delivery and a full Technical Specification for your individual Project please contact:

Property Repair Systems, Unit 3 Olympus Business Park, Kingsteignton Road, Newton Abbot, Devon TQ12 2SN

Tel: 01626 331351  Fax: 01626 331143

E Mail: help@propertyrepairsystems.co.uk